Preparation And Studies The Electrical And Magnetic Characteristic  For The System

Nix Zn(1-x-y)CuyFe2O4

Mustefa Afuony, M.A. Batal , Nahedh.H.Alwash. *

Dept. of physics college of science university of Aleppo,*Postgraduate Student(PhD)

Abstract

The Conventional Solid State  reaction is used to prepared  the  (ZnFe2O4  ,NiFe2O4  ,CuFe2O4) From  the Oxide of (Cu,Zn,Ni & ferrous oxalate) while had emphasized the Crystallize  Synthesis  accurately  and Sort  by  these  Synthesis  by  using the  Technique (X.R.D) , it is  mixed to Formed the final Synthesis (Nix Zn(1-x-y)CuyFe2O4) with (x= 0.1,0.3 ,0.5, 0.7) & (y=0.2)as pressed pellets for electrical properties studies and rings  for magnetic characterization studies ,by hydraulic press (3tons ) then are sintered at (1250)C˚ for (2h) bulks densities and electrical characteristic are measured . The electrical characteristics for pellets samples, included the measure of D.C current as electrical resistivity (r) and A.C current as the measure of dielectric constant (e¢),the magnetic characteristics included the measure the magnetic permeability μ) I (,the studies are show that the x increase lead to decreasing in density ,decreasing resistivity value to x=0.3 then it will be increase ,the dielectric constant depends on frequency and so on the magnetic permeability μ) I (